## Slide 1
Tower CONNECTIONS
Michelle Kleinau
02/18/2019

## Slide 2: ANCHOR BOLTS
#11 ASTM A615 Grade 75 – per RRC SE1810019 S-2

## Slide 3: TENSION PROCEDURE
Requirements – per RRC SE181001
  Min grout strength prior to tension: 3,500 psi (RRC S-7)
  Post-tension: 45 kips +10/-0 kips tolerance (RRC S-4)
In Application:
  Desired elongation: 0.1”
  Pressure setting: 3,500 psi

## Slide 5: TENSION REPORT

## Slide 6: TOWER SPLICE BOLTS
Per Agbayani HH80M-00.20.4.305.24-ver2C

## Slide 7: SPLICE DETAILS

## Slide 8: TORQUE GUIDE

## Slide 9: TORQUE REPORT

## Slide 10: Questions?